# PRODUCT SPECIFICATION FOR SINGLE STRIP 145MM (5 ¾”) / TUFFLOC

| Criteria | Applicable Standard | Nominal Value / Tolerances |
| --- | --- | --- |
| A. Product |  |  |
| 1. Length | - | 1820 +/- 5mm |
| 2. Width | - | 145 +/- 0.1mm |
| 3. Total Thickness | - | 14.20 +/- 0.1mm |
| 3.1 Top Layer | - | 3.2 +/- 0.1mm |
| 3.2 Core Layer | - | 9 +/- 0.1mm |
| 3.3 Bottom Layer | - | 2 +/- 0.1mm |
| 4. Squareness | prEN 175054, DIN280-1 | = 0.1% along width |
| 5. Diagonal Curve | prEN 175054, DIN280-1 | = 0.1% along width |
| 6. Straightness | prEN 175054, DIN280-1 | = 0.1% along length |
| 7. End lamella length | - | = Full Piece Single Face |
| 8. Moisture Content | - | 7% +/- 1% |
| 9. Adhesive |  | CASCO ADHESIVES / Urea Formaldehyde System |
| 10. Scratch resistant | KLUMPP | 7 coats |
|  |  | Abrasion Resistance > = 6000 revolutions ASTM D 4060 (CS17) |
| 11. Ceramic (Aluminium Oxide) | KLUMPP | 7 coats |
|  |  | Abrasion Resistance > = 25000 revolutions ASTM D 4060 (CS17) |
| 12. Oil | KLUMPP | 1 or 2 sealer oil and 1 top oil |
| 13. Gloss Level | Gloss meter, 60’ angle | 8%, 30%, 45% or 65% gloss |
| 14. Formaldehyde Emission | EN 717-1 | ≤ (less than or equal to) 0.1mg formaldehyde/m3 air |
| B. Packaging |  |  |
| 1. Pieces per set |  | 6 |
| 1.1 Packaging material | - | Wrapped with shrinking transparency. Includes colour insert / Flyer / Laying Instructions |
| 2. Set per pallet and number of pallets per 20’ container | - | 77 packs @ 6 large pallets & 66 packs @ 6 small pallets, total of 12 pallets |
| 2.1 Packaging material | - | As per request |
| 3. Flyer (including instruction manual) | - | According to films provided |
| 4. Additional information on packaging | - |  |
| 4.1 Shipping mark | - | 4 sides shipping marks |
| 5. Nesting Policy |  | Minimum 1 piece every 6 pieces (1 pack) |